## Slide 1: Shear Viscosity of Colloidal Suspensions

## Slide 2: Simulated System
Implemented a shearing DPD simulation with equations and dynamics from Pryamitsyn
Viscosity is calculated with a Lees-Edwards system, shear stress is computed and then the integral of this stress autocorrelation function is computed

## Slide 3: Simulated System

## Slide 4: Interaction Forces
DPD Forces between fluid particles
  Inclusive of rotation – Each particle has a velocity and also an angular velocity
  Particles can exert off-axis forces and torques on one another
Lennard-Jones potential for fluid-colloid and colloid-colloid pairs
  Fluid-colloid potential is much softer than the colloid-colloid pairs

## Slide 5: Interaction Forces

## Slide 6: Calculation of Viscosity
Viscosity is calculated using the formula:
Where

## Slide 7: Calculation of Viscosity
Therefore:
Where:
Hence:

## Slide 8: Variation of Shear Rate
Chart: Average Viscosity
| 1E-3 | 3.0000000000000001E-3 | 0.01 | 0.03 | 7.0000000000000007E-2 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 1 | 1.5 | 2 | 2.5
Visc_avg | 4.1042 | 4.0668 | 4.1879 | 4.0322 | 4.1107 | 4.1861 | 4.1781 | 4.3259 | 4.4019 | 4.5725 | 4.6924 | 4.803 | 5.1536 | 4.9119 | 5.1877 | 5.11 | 6.0336 | 7.9041 | 10.7172 | 14.0971
Chart: Translational Temperature
| 1E-3 | 3.0000000000000001E-3 | 0.01 | 0.03 | 7.0000000000000007E-2 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 1 | 1.5 | 2 | 2.5
Trans_avg | 1.0029 | 1.0013 | 1.0033 | 0.99873 | 1.0022 | 0.9979 | 0.99975 | 1.0061 | 1.0028 | 1.0074 | 1.0118 | 1.0109 | 1.0245 | 1.0204 | 1.0359 | 1.022 | 1.0355 | 1.0869 | 1.1566 | 1.2461
Chart: Average Viscosity
| 1E-3 | 3.0000000000000001E-3 | 0.01 | 0.03 | 7.0000000000000007E-2 | 0.1 | 0.2 | 0.3 | 0.4
Visc_avg | 4.1042 | 4.0668 | 4.1879 | 4.0322 | 4.1107 | 4.1861 | 4.1781 | 4.3259 | 4.4019
Temperature is constant
as long as
Viscosity is constant within
this regime.

## Slide 9: Viscosity Measurements

## Slide 10: Variation with particle number
Shear Rate: 0.1
Viscosity peaks sharply as we approach maximum packing density
Chart: Norm Viscosity against Fill Fraction
| 0 | 5.9573905134739778E-2 | 0.11914781026947956 | 0.17872171540421933 | 0.23829562053895911 | 0.29786952567369884 | 0.35744343080843866 | 0.41701733594317847 | 0.47659124107791823 | 0.53616514621265798 | 0.55602311459090459 | 0.57588108296915119 | 0.59573905134739769 | 0.6155970197256444 | 0.63545498810389089 | 0.6553129564821375 | 0.6751709248603841 | 0.69502889323863071 | 0.71488686161687731 | 0.73474482999512392 | 0.75460279837337052 | 0.77446076675161712 | 0.79431873512986362 | 0.81417670350811022 | 0.83403467188635694 | 0.85389264026460354 | 0.87375060864285004 | 0.89360857702109664 | 0.91346654539934324 | 0.93332451377758974 | 0.95318248215583645 | 0.97304045053408306 | 0.99289841891232966 | 1.0127563872905763
V_norm | 1 | 1.4306 | 2.0359 | 2.9121 | 3.9474 | 6.1405 | 4.8648 | 11.6196 | 16.4581 | 24.4622 | 25.1786 | 21.1673 | 27.9133 | 34.6468 | 41.9627 | 66.6717 | 73.0555 | 99.8627 | 107.8842 | 114.4421 | 170.0866 | 204.7857 | 248.3109 | 368.8057 | 333.753

## Slide 11: Variation of Repulsion Parameter
Chart: Normalised Viscosity against Fill Fraction
| 0 | 0.65934660630896891 | 0.67873915355335046 | 0.69813170079773179 | 0.71752424804211334 | 0.73691679528649467 | 0.75630934253087612 | 0.77570188977525756 | 0.795094437019639 | 0.81448698426402044 | 0.83387953150840188 | 0.85327207875278333 | 0.87266462599716477 | 0.8920571732415461 | 0.91144972048592765 | 0.93084226773030909 | 0.95023481497469053 | 0.96962736221907198
Epsilon = 550 | 1 | 123.3078 | 112.0713 | 156.7602 | 209.1388 | 126.5083 | 195.8271 | 195.655 | 267.6976 | 211.6989 | 548.2164 | 459.284 | 456.8735 | 764.5143 | 998.5624 | 1050.4511 | 1310.6351 | 2170.1322
Epsilon = 110 | 1 | 1.2941 | 1.9524 | 3.0825 | 4.5127 | 6.3889 | 8.2639 | 10.9373 | 14.6797 | 18.3275 | 23.3663 | 28.4454 | 29.0464 | 30.4294 | 38.6706 | 39.1938 | 39.9164 | 44.7757 | 46.7053 | 48.792 | 59.0006 | 65.2216 | 69.1881 | 76.8715 | 103.603 | 101.562 | 120.9462 | 133.7388 | 172.0846 | 183.1887 | 232.3439 | 267.6677 | 335.2126 | 349.8332 | 388.382
Increasing repulsion parameter increases viscosity
due to increased interaction forces

## Slide 12: Variation of particle size
Chart: Norm Viscosity against Fill Fraction
| 0 | 5.9573905134739778E-2 | 0.11914781026947956 | 0.17872171540421933 | 0.23829562053895911 | 0.29786952567369884 | 0.35744343080843866 | 0.41701733594317847 | 0.47659124107791823 | 0.53616514621265798 | 0.55602311459090459 | 0.57588108296915119 | 0.59573905134739769 | 0.6155970197256444 | 0.63545498810389089 | 0.6553129564821375 | 0.6751709248603841 | 0.69502889323863071 | 0.71488686161687731 | 0.73474482999512392 | 0.75460279837337052
Particle Radius = 2 | 1 | 1.4306 | 2.0359 | 2.9121 | 3.9474 | 6.1405 | 4.8648 | 11.6196 | 16.4581 | 24.4622 | 25.1786 | 21.1673 | 27.9133 | 34.6468 | 41.9627 | 66.6717 | 73.0555 | 99.8627 | 107.8842 | 114.4421 | 170.0866
Particle Radius = 2.5 | 1 | 1.7163 | 2.3746 | 4.5979 | 5.3916 | 4.8767 | 13.6654 | 11.9777 | 19.8429 | 35.4146 | 47.5446 | 63.0238 | 90.322 | 67.6571 | 73.921 | 103.6935 | 87.0982 | 192.1389 | 148.6971 | 205.763
Weak effect of changing size of particles while keeping fill fraction constant

## Slide 13: Mixed Particle Sizes
Chart: Norm Viscosity against Fill Fraction
| 0 | 5.3261553436504648E-2 | 0.1065231068730093 | 0.15978466030951394 | 0.21304621374601859 | 0.26630776718252325 | 0.31956932061902787 | 0.3728308740555325 | 0.42609242749203718 | 0.47935398092854181 | 0.50598475764679418 | 0.53261553436504649 | 0.55924631108329881 | 0.58587708780155112 | 0.61250786451980332 | 0.63913864123805575 | 0.66576941795630817 | 0.69240019467456038 | 0.71903097139281269 | 0.745661748111065 | 0.77229252482931743 | 0.79892330154756963 | 0.82555407826582194 | 0.85218485498407437 | 0.87881563170232668 | 0.905446408420579 | 0.9320771851388312 | 0.95870796185708362 | 0.98533873857533605 | 1.0119695152935884 | 1.0386002920118405 | 1.065231068730093 | 1.0918618454483453 | 1.1184926221665976
1.8 and 2.5 particles | 1 | 1.5934 | 1.9804 | 4.2827 | 3.549 | 6.1005 | 4.3831 | 9.3046 | 22.103 | 13.6726 | 23.3776 | 25.1207 | 24.9373 | 43.7441 | 27.9423 | 66.4682 | 71 | 74.9768 | 86.3629 | 113.3974
2.5 particles only | 1 | 1.7163 | 2.3746 | 4.5979 | 5.3916 | 4.8767 | 13.6654 | 11.9777 | 19.8429 | 35.4146 | 47.5446 | 63.0238 | 90.322 | 67.6571 | 73.921 | 103.6935 | 87.0982 | 192.1389 | 148.6971 | 205.763
Weak effect of having a mixture of particle sizes

## Slide 14: Colloid Particle Geometry

## Slide 15: Fill Fraction

## Slide 16: Coordination Number
Chart: 
| 0.29088820866572157 | 0.40724349213201022 | 0.52359877559829893 | 0.63995405906458758 | 0.69813170079773179 | 0.75630934253087612
Coordination Number | 1.2 | 2.2857 | 4.07 | 5.3939 | 6.2778 | 6.718

## Slide 17: Bond Angle
Fill Fraction: 0.41
Coordination Number: 2.3
Fill Fraction: 0.52
Coordination Number: 4.1
Fill Fraction: 0.76
Coordination Number: 6.7

## Slide 18: Shear Rate